PROPYLENE

According to GOST: 25043-87

Технические характеристики

| Technical Parameters and indicators | Parameters |
| --- | --- |
| Propylene content, not less than [%] | 99,8 |
| The volume fraction of ethylene, not more than [%] | 0,005 |
| The volume fraction of acetylene and methyl acetylene, not more than [%] | 0,001 |
| The volume fraction of C4 hydrocarbons, not more than [%] | 0,002 |
| The volume fraction of diene hydrocarbons (propanediamine and butadiene), not more than [%] | 0,001 |
| The volume fraction of methane, propane, not more [%] | 0,2 |
| The mass concentration of sulfur, not more [mg/m3] | 1 |
| Mass fraction of water, not more [%] product supplied in tanks | 0,02 |
| The content of free water | absence |